LymTal International, Inc.

Waterproofing Products

Guide Specification

Section 07102

ISO-FLEX PRECOM V PRE-COMPRESSED JOINT SEAL

EXPANSION JOINT SYSTEM

## PART 1 – GENERAL

  - WORK INCLUDED

The work shall consist of furnishing and installing expansion joints in accordance with the details shown on the plans and the requirements of the specifications.

  - SUBMITTALS

- Template Drawings – Submit typical expansion joint cross section(s) indicating pertinent dimensioning and relationship to adjacent trades.

## PART 2 – PRODUCTS

  - MATERIALS

The joint seal shall be composed of a pre-compressed polyurethane, microcell foam waterproofed with a hydrophobic polymer compound that is UV stable and chemically resistant.  The design of the seal shall accommodate movements and differences in the joint widths through compression of itself.  The system shall utilize a self-adhesive tape to aid in the installation of the seal.

For horizontal and vertical expansion joints furnish Iso-Flex Precom V Seal System as manufactured by Lymtal International (248) 373-8100 and as indicated on drawings.  Select the appropriate size of the seal based upon project conditions.

  - COMPONENT PROPERTIES

- Pre-compressed Seal

Provide seal as specified and indicated on the contract drawings.  Seal material shall meet the following physical properties indicated below:

### PHYSICAL PROPERTIES – “Precom V” SYSTEM

PRE-COMPRESSED JOINT SEAL

Physical Properties			Requirements

A.  Material 				Polyurethane Foam

B.  Density				5.5-6.5 lb./cu. ft.

C.  Thermal Conductivity			0.28-0.30 Btu-in/hr-°F-ft2

D.  Temp. Stability Range    		 -40°F to 194°F (-40°C to 90°C)

E.  Staining/Bleeding                    	DIN 18542, meets DIN req.

F.  Tensile Strength                		ASTM 3574, meets 21 psi min.

G.  Elongation                                  	ASTM 3574, 120% ±20%

H.  Resistance to

Compression Set                           	ASTM 3574, Max 4.2%

I.   Mildew Resistance	                  	Excellent

J.   Staining	                         None

K.  Fire testing            			ASTM E 84, Flame spread 0, Smoke 5

L.  Fire testing            			ASTM E 84, Flame spread 0, Smoke 5

  - Fabrication

- Seal profiles shall be shipped Pre-compressed.  Seals shall be cut to length and mitered on jobsite where required.

  - Finishes

- Seals – Color:  Black or gray

PART 3 – EXECUTION

  - General

All work shall be performed in clean, dry, sound expansion joint gap openings.

  - Preparation

- The contractor shall provide properly formed, solid joint gaps with clean, sound substrate and in accordance with the dimensions detailed in the drawings.

- Work shall not proceed under adverse weather conditions or when temperatures are outside the manufacture’s recommended ranges.

  - Installation

- The installation of the expansion joint system shall be completed in strict accordance with the manufacturer’s recommendations.

- Expansion joint systems shall be stored in a cool place prior to placement to give the installer sufficient time for placement in extreme heat conditions.

  - Clean and Protect

Protect the Iso-Flex Precom V Pre-compressed Seal System during construction.  Heavy construction vehicles will not be permitted to cross the joint without specific and written permission by the engineer.  Subsequent damage to the expansion joint system shall be repaired at the contractor’s expense.

-end-